## Slide 1: Using Electrochemical Simulation to both Optimize Alloy Electroplating and Predict the Consequent Impact on Product Corrosion Resistance
Alan Rose Ph.D., Siva Palani Ph.D., Keith Legg Ph.D., Ashok Vaishnav Ph.D., Julio Mendez Ph.D.

## Slide 2: Agenda
Problem
  Replacement of hazardous corrosion resistant coatings
  Transition challenges
Modeling Approach
Simulations
  Plating
  Corrosion
  Validation & Verification
Summary

## Slide 3: Simulations show the WHAT and HOW
WHAT
  evaluating what we need in the field to achieve product corrosion resistance
HOW
  optimizing manufacturing process to establish how the correct coating should be plated

## Slide 4: The Corrosion Problem
Cost
Safety
Readiness
Annually
The NACE 2016 IMPACT study estimates the global cost of corrosion to be $2.5 trillion which is equivalent to 3.4% of the global gross domestic product (2013).
It is estimated that savings of 15%-35% of this cost could be realized by implementing corrosion control and better design practices.
  $20.9bn
  25 days unavailable

## Slide 5: Harsh environments - USS Kitty Hawk
https://youtu.be/Z0Jzb8dfcC4

## Slide 6: F-18 wing and airframe corrosion
NAVAIR Public Release SPR-2012-982
More than 80% of military aircraft structural failures are initiated from corrosion pits
Repair: remove corrosion and bush hole with PH stainless; now corrodes around bushing. Ti bushings usually a big improvement over stainless.

## Slide 7: Landing gear corrosion
www.flightsafetyaustralia.com
17 Jan – 25 March 2014

## Slide 8: Anatomy of a landing gear
https://core.ac.uk/download/pdf/14697838.pdf

## Slide 9: Drag brace
Lower drag brace Main LG
https://upload.wikimedia.org/wikipedia/commons/thumb/4/49/U.S._Marine_Corps_F-35B_Lightning_II%28169164%29_of_VMFA-121_right_main_landing_gear_right_front_view_at_MCAS_Iwakuni_May_5%2C_2018_02.jpg/400px-U.S._Marine_Corps_F-35B_Lightning_II%28169164%29_of_VMFA-121_right_main_landing_gear_right_front_view_at_MCAS_Iwakuni_May_5%2C_2018_02.jpg

## Slide 10: Cd replacement with ZnNi – sacrificial protection
REACH - Registration, Evaluation, Authorisation and Restriction of Chemicals
EOSH - Environmental and Occupational Safety and Health
EPA – Environmental Protection Agency
Replacement with ZnNi
  Thickness distribution
  Composition

## Slide 11: Factors known to affect Ni content in ZnNi alloy

## Slide 12: Impact of ZnNi composition
Alkaline LHE ZnNi chemistry and corrosion resistance as a function of wt% Ni. (Bjorn Dingwerth, Atotech, SURFIN (2012).

## Slide 13: Modeling approach - electrochemistry
Primary Current Distribution accounts solely for electrical transport losses due to resistance. These simulations refrain from solving species concentrations. When temperatures are fixed only one (PDE) is solved for the electric potential, thus reducing the computational effort significantly. Neglecting activation overpotentials corresponds to assuming an infinite electrochemical reaction rate where all significant losses occur in the electrolyte and/or in the metal transport of charge carriers.
Secondary current distribution setups build on primary current distribution, but additionally account for activation overpotentials. These simulations do not resolve species concentrations, assuming a perfectly mixed electrolyte.
Tertiary Current Distribution the most detailed modelling approach, where reaction rates and overpotentials are concentration dependent requiring the highest computational effort. For isothermal tertiary, one PDE is solved for each species. These PDEs depend on flow velocities, so, three additional equations are solved for U, V, W plus pressure, in addition to the PDE for electric potential. Thus, the tertiary setup requires solution of at least 5+n PDEs, whereas the primary and the secondary setups are required to solve only one.
Siemens Star CCM+ v2019.2
https://www.plm.automation.siemens.com/global/en/products/simcenter/STAR-CCM.html

## Slide 14: Modeling approach - plating
Gather solution data – Hull cell experiments
  Anodic & cathodic data
  Plating efficiency
CAD geometry of plating tank
Insert CAD geometry of component to be plated

## Slide 15: Hull cell – plating data
Chart: Efficiency (A/m2)
| 50 | 100 | 200 | 400 | 800
 | 53 | 47 | 42 | 37 | 28
Corrdesa Hull cell model
cathode
anode
www.yamamoto-ms.co.jp

## Slide 16: Landing gear in plating tank
https://www.lufthansa-technik.com/documents/5875801/6300210/090910_Galvanik++64461_16x9.jpg/692b1cb1-a8f5-4d66-bea3-2f1089e45908?t=1539967084906

## Slide 17: Surrogate geometry and plating tank
Representative auxiliary anode tooling, assumed connected to main power supply.
Other auxiliary anodes not included
Tank anodes
Surrogate
drag brace

## Slide 18: Thickness variation

## Slide 19: ZnNi thickness & composition with auxiliary anode
Very important: Low current density gives low thickness with high Ni%

## Slide 20: Post plating measurement
XRF measurement confirms Ni content within 12-16% range, BUT
  Variations on edges and in recesses
  Cannot measure locations where thickness and Ni% vary most
Better QA if can relate to the worst or most sensitive areas
Beware: Some aerospace materials contain Ni, which can affect measurements, such as A100 is 11% Ni, 300M is 1.8% Ni
Within allowable range

## Slide 21: Modeling approach - corrosion
Gather material polarization data – potentiostat expt
  Anodic & cathodic data
CAD geometry of component
Wrap CAD component in fluid shell (electrolyte film)
  3.5% NaCl solution to represent maritime
  5% NaCl solution to represent ASTM B117 chamber

## Slide 22: Polarization curves
Ti/Al
SS/Al
ΔE Ti/Al
ΔE SS/Al
Despite the potential difference between Ti/Al being larger than that between SS/Al, the SS galvanically corrodes the Al at an order of magnitude faster rate.

## Slide 23: Maritime environment
25oC

## Slide 24: Chamber environment

## Slide 25: ZnNi polarization for different Ni content
Less noble ZnNi

## Slide 26: ZnNi plated Aermet 100 – with defect
For the more noble ZnNi the average potential of the exposed Aermet 100 in the defect is -776mV (just 46 mV below its OCP) compared to -945mV (215mV below OCP) in the case of the less noble ZnNi coating.
What this means is that the less noble ZnNi coating brings down the Aermet potential 215mV (on average) below its OCP, firmly placing the material into the cathodic region and protecting it ‘cathodically’.
Whereas, the more noble ZnNi only brings down the Aermet potential by 46mV, providing little protection.
More noble ZnNi
Less noble ZnNi

## Slide 27: Impact of Ni varying composition
More noble ZnNi provides less protection… where more strength is required!
So this could be addressed by design and placement of auxiliary anodes

## Slide 28: Verification & Validation
Plating
  Hull cell measurements
  also can measure thickness and composition on actual plated components (proprietary data)
Corrosion
  Controlled beach and environmental chamber
  Measurements from actual field components

## Slide 29: Hull cell: Comparing prediction and measurement
Without plating efficiency
Implementing plating efficiency term
Experimentally measured data points (in blue)

## Slide 30: ASTM B117 vs Fielded Coupons
Z. Feng, G.A. Frankel, W.H. Abbott, C.A. Matzdorf, “Galvanic Attack of Coated Al Alloy Panels Laboratory and Field Exposure”, Corrosion 72 (2016); p. 342.
Fastener corrosion current µA
Fastener corrosion current µA

## Slide 31: Current density & corrosion

## Slide 32: Model comparison
Chamber
Beach
Fastener corrosion current µA
Fastener corrosion current µA

## Slide 33: Summary
Corrosion is a cost and safety issue. Many coatings are hazardous and are presently being replaced
Cd is toxic sacrificial coating and can be replaced with ZnNi
ZnNi, being an alloy is more difficult to plate but simulation can establish optimum parameters
Corrosion simulation can then assess corrosion resistance of the plated coating
What does it mean for OEMs?
Supplier setup qualification
  Define allowable thickness/chemistry variations, QC locations
  Check validity of plating set up to stay within allowables
    Including auxiliary anodes and chemistry maintenance
QC/QA
  Define test locations – thickness, Ni%
  Establish consistency across supplier network

## Slide 34: Thank You!
Alan Rose, Corrdesa LLC, Tyrone, GA, USA
arose@Corrdesa.com
770 683 3960